## Slide 1
Challenge Information Packet
On
Residual Stress Measurement Results
Last updated: 07/08/2020
Nicholas A. Bachus (nabachus@ucdavis.edu)
Christopher R. D’Elia (crdelia@ucdavis.edu)
Professor Michael R. Hill (mrhill@ucdavis.edu)
UC Davis Team
ORNL Team
Sougata Roy (roys1@ornl.gov)
Jason Allen (allenjp@ornl.gov)
Yan Chen (cheny1@ornl.gov)
Ke An (kean@ornl.gov)
Andrzej Nycz (nycza@ornl.gov)
Luke Meyer (meyerlt@ornl.gov)

## Slide 2: Introduction
These charts contain a summary of residual stress measurement data for Metal Big Area Additive Manufacturing (MBAAM) calibration builds
  Residual stress data are available in a separate file
  \SRP\SRPCALLPackage\ResidualStress\CalTask\Residual Stress _calibration sample.xlsx
A companion document provides a summary of the procedures used to gather residual stress data
  ORNL_MBAAM_Challenge_Residual_Stress_Measurement_Procedures_V0.pptx

## Slide 3: Measurement tracking scheme
Distance to cut/measurement plane
  Along the direction from origin of the build
Measurement identifier
  Sample - stress component direction - location of measurement as a length (millimeters) along direction - measurement type
  Example: CAL1-SYY-Neg125mm-CM
    Translation: Calibration Sample 1, measurement of YY stress, at from the origin using contour method (CM: contour method, ND: neutron diffraction)
LB
WB
W
L
sy
Measurement plane
Y
X
Build
Baseplate

## Slide 4: CAL1-SYY-0mm-CM (mid-plane)
Bisecting cut on CAL1 at at
  Voids and inclusions within the build caused issues when cutting the part which subsequently introduced cutting artifacts on the deformed surface
  Stress computed with possible plasticity artifacts excluded from figure
  At the center of the sample, moving along the direction and starting at , the stress varies from to (, down to at roughly the center of the baseplate (, back to at the bottom surface (
Cut 2
Cut 1
Cutting artifacts
Potential plasticity artifact
Potential plasticity artifact

## Slide 5: CAL1-SYY-Neg125mm-CM (quarter-plane)
Quarter-plane cut on CAL1 at
  Slag on surface of sample caused the cut to be interrupted and created the cutting artifact
  Stress computed with possible plasticity artifact excluded from figure
  Along the center of the sample, moving from the top of the build () to the bottom of the baseplate, the stress varies from to (), down to at roughly the center of the baseplate (, back to at the bottom surface (
Self-constraint holes
Cut 3
Cut 2
Cut stopped due to surface slag
Cut 1
Potential plasticity artifact
Notes: Add picture of as cut surface state

## Slide 6: CAL1-SXYZ-0mm-ND (mid-plane)
  to variation from top to bottom
  to variation from top to bottom
  : to variation from top to bottom
Measured three components of residual stress via neutron diffraction on the plane bisecting the origin (): Transverse (X), Longitudinal (Y), and Build (Z)
X
Y
Neutron diffraction measurement region

## Slide 7: CAL1-SXYZ-Neg125mm-ND (quarter-plane)
Neutron diffraction measurements in the negative Y region at from the sample origin
  to variation from top to bottom
  to variation from top to bottom
  : to variation from top to bottom
X
Y
Neutron diffraction measurement region

## Slide 8: CAL1-SXYZ-Pos125mm ND (opposing quarter-plane)
Neutron diffraction measurements in the positive Y region at from the sample origin
  to variation from top to bottom
  to variation from top to bottom
  : to variation from top to bottom
Neutron diffraction measurement region
X
Y

## Slide 9: CAL1 residual stress measurements
Neutron diffraction area is a subset of the contour measurement area
Contour method (CM) magnitudes are generally lower than the neutron diffraction (ND) magnitudes
  CAL1-SYY-0mm max stress: Contour = 380 MPa, Neutron = 500 MPa
  CAL1-SYY-Neg125mm max stress: Contour = 280 MPa, Neutron = 425 MPa
Similar trends
  High tension at the top of the baseplate, then approaches 0 MPa as you move towards the top of the build
Contour
Neutron Diffraction
Quarter-plane
Mid-plane
Plasticity artifact removed

## Slide 10: Lineouts using boxcar averaging volume
Using boxcar averaging routine for CM and ND measurements, with the error bars representing the standard deviation of points within the boxcar volume
  Horizontal Lineouts
    Boxcar volume 2 mm ( dimension) x 2 mm ( dimension) – 2 mm was chosen since the largest variations are seen along the height of the sample and we did not want to obscure the horizontal lineouts with this variation
    2 mm spacing along X direction
  Vertical lineouts
    Boxcar volume 15 mm ( dimension) x 2 mm ( dimension) - 15 mm was chosen to provide a representation of residual stress averaged across several of the beads in the weld deposit, near the build center
    2 mm spacing along Z direction
Boxcars for vertical lineouts
(15 mm x 2 mm)
Boxcars for horizontal lineouts
(2 mm x 2 mm)

## Slide 11: CAL1 lineouts
Horizontal lineout boxcar volumes 2 mm x 2 mm
Vertical boxcar volumes 15 mm x 2 mm
Discontinuities in contour method lineouts represent removed potential plasticity error regions
See similar trends in the vertical lineouts between the contour method and neutron diffraction residual stress measurements with the neutron diffraction magnitudes being roughly 2x as large as the contour method